Victorian Post Sleeve and Base

Specifications

Sleeve:  Series 6000 or greater, hardened extruded aluminum, alloy #6063-T6.  Dimensions 3.050” x 42” (2.550” ID, 3.050” OD, outside flute radius .330R, inside flute radius .280R.  Weight: 4.5# min.  Sleeve should be 3/16” shorter than the above-ground length of the parking meter post.  It may be 1-2” shorter if height adjustment screws are utilized.  Sleeve may be trimmed on-site using a chop saw with diamond tipped cutting blade or comparable.

Decorative base:  Die-cast non-ferrous #319S certified aluminum alloy.  Dimensions: 7.375” x 4.25” (7.375” OD, 6.625” ID, outside flute radius .330R, inside flute radius .280R.  Weight 3.25# min.  Includes (3) 1/4-20x3.8 stainless steel height adjustment set screws.

Finish:  electrostatically painted with TGIC polyester powder paint in standard dark gray color or gloss black, and baked to withstand ASTM B117 1000-hour salt spray test.  Optional colors are available.

Design must match attached photo image to ensure continuity of design with sleeves and bases already installed at this location.